## Slide 1: CLIC RF structure master schedule and CERN production
10.07.2010

## Slide 2
Structure master schedule
#1, SFO on 23.06.2009 (tank version) #2 LT Ultra disks W27 (sealed version)
#1 non conform
#2 available
CD10
- Prototype phase (P) for 4 different material (Kugler, LT Ultra)
- Full structure in OFE at VDL
Cooling circuits shipped to SLAC
Installation started in cw27
swapped
Bars at CERN
Decision to cut a T18

## Slide 3
Structure master schedule
Fabrication at Kugler:
#1 received in April NC,
#2 required - prototype disk OK
    disks at CERN CW28
Fabrication at VDL:
#1 and #2 disks finished
disks at CERN

## Slide 4
SLAC/KEK technology,
KEK copper disks CW31
Structures in the pipeline
Missed slot in ASTA, back to CERN?
Stand-by

## Slide 5
2nd unit, preparation in stand-by
Contract with KEK signed on 19.06, design started
T24 with smaller D and new tuning features
Under tendering
Mode launcher coupler, symm. disks
J. Huopana, disks for brazing test cw28
Compact coupler, asymm. disks
Ridged waveguides

## Slide 6
Mechanical design
started
Mechanical design
not started yet

## Slide 7
Radial choke damping
Lower DT
Other structures:
x-band speed bump structure
CLIC K structures
500 GeV structures

## Slide 8: T24#1 (tank version)
Vacuum baking
4 h at 650 °C
Red: changes wrto previous assembly procedure

## Slide 9: TD24 #1
RF check  non conform
Inspection of all disks (see EDMS report: 10006094
Brazing material inside the disks
Launched program to qualify assembly procedure (aim bonding at 1000 C)
First results with pure bonding on two samples of 5 disks each seem to be promising